Swiss III Technical Specification

|  |  |  |
| --- | --- | --- |
| SWISSseries | Fabric | 100% polyester warping knit |
| Coating | Poly urethan / Acylics |
| Width | 94 inch |
| Thickness | 0.35mm (±5%) |
| weight | 150g/m2(±5%) |